Po06

HYDROTREATING OVER SILICA-ALUMINA SUPPORTED CATALYSTS
Daniela Gulková, Zdeněk Vít, Luděk Kaluža

Institute of Chemical Process Fundamentals of the ASCR, v.v.i.
Rozvojová 135, 165 02 Prague 6, Czech Republic,

Hay

PdPt catalysts on acidic supports show high efficiency in aromatics hydrogenation. They are studied for possible use in deep hydrodesulfurization (HDS)1 while they have not been investigated for the HDS parallel with hydrodeoxygenation (HDO)2. The aim was to find the effect of active phase and support of Pd and PdPt catalysts on activity and selectivity in HDS of 4,6-dimethyldibenzothiophene (DMDBT) and HDS/HDO of l-benzothiophene/octanoic acid (BT/OA). Supported sulfided CoMo or NiMo phase was chosen as the standard for comparison of activity and selectivity. Precipitated mesoporous SiCH-AhO) was dealuminated3 and impregnated with active metals (Table 1). Catalyst activities were evaluated in fixed bed flow reactors2,3 and they were expressed by pseudo first order rate constants (/c) of DMDBT consumption and ethylbenzene,liquid hydrocarbons Ifui.HDsIkLHC.HDo) formation in Table 1.

Table 1. Activity in I IDS of DMDBT (Ły-Uö»r) and HDS/HDO of BT/OA (Âra. kLHC\

Catalyst composition (wt. %)	Catalyst actix ity k (mmol/h.gCiU)

The m<i ir.ea ef:o

| Active metals | AI2O3 in SÍO2-AI2O3 | koMDBT | k Etl.ltos | ki.nc.Hix> |
| --- | --- | --- | --- | --- |
| Pd | 0.31 | 2 | 9.6 |  | - |
| Pd | 0.35 | 8 | 4.4 |  | - |
| Pd | 0.35 | 12 | 2.4 |  | - |
| PdPt | 0.10 | 2 | 7.1 |  | - |
| PdPt | 0.32 | 2 | 19.3 | 51 | 33 |
| PdPt | 0.82 | 2 | 21.7 |  |  |
| PdPt | 1.23 | 2 | 23.2 |  |  |
| PdPt | 0.11 | 4 | 10.2 |  |  |
| PdPt | 0.3! | 9 | 15.8 |  |  |
| PdPt | 0.74 | 13 | 14.1 |  |  |
| PdPt | 1.32 | 13 | 30.3 |  |  |
| PdPt | 1.50 | 13 | 22.3 | 30 | 16 |
| CoMo | 16.3 | 13 | - | 21 | 99 |
| NiMo | 16.3 | 13 | - | 27 | 158 |
| Commercial 12.9 wt.%(Co+Mo)/Al2Ü3 | 1.5 | 30 | 97 |

Pd and PdPt catalysts were more active than CoMo in HDS of DMDBT and
HDS proceeded over them entirely by HYD route. CoMo and NiMo were highly active
towards formation of liquid hydrocarbon (kutc.Hool while PdPt catalysed cracking to
gaseous hydrocarbons during HDS/HDO of BT/OA.

Acknowledgement. The financial support of the Czech Science Foundation
(grant No. 17-22490S) is gratefully acknowledged.

References:

Niquille-Röthlisberger, A.; Prins, R. Catal. Today 2007, 123, 198-207.

Kaluža. L; Karban, J.; Gulková, D. React. Kinet. Catal. Lett. 2019, 127, 887-902. Vít. Z.; Gulková. D.; Kaluža, L.; Kupčík, .1. Appl. Catal. B 2015, 179,44-53.

51th Symposium on Catalysis. November 4-5, 2019