Po20

Co-Mn MIXED OXIDES PREPARED BY MAGNETRON SPUTTERING ON

MESHES AS CATALYSTS FOR OXIDATION OF ORGANIC COMPOUNDS

Kvčta Jirátová“, Roman Perckrestov6, Michaela Dvořáková*. Jana Balabánová",
Martin Koštejn“, Pavel Topka", Petra Kšírová1*, Martin Čada1', Zdeněk Hubička11,
František Kovanda*

1 Institute of Chemical Process Fundamentals oj the CAS, v. v. i.. Rozvojoví) 135. 165 02
Prague, Czech Republic

• Institute of Physics of the CAS. v.v.L. Na Slovance. 1999/2. 182 2/ Prague, Czech
Republic.

J University of Chemistry and Technology, Prague. Technická 5, 166 28 Prague.

Czech Republic

Catalysts in the form of meshes show low pressure drop and good heat transfer. Oxides of Co and Mn. active in various oxidation reactions, were prepared as follows: Stainless steel meshes used as supports were coated with thin CO3O4 film by RF magnetron sputtering and further Co.iO-i layer by subsequent electrochemical deposition followed by heating. The meshes with deposited CoiO-i were then coated with additional MnO (samples A-C) or Co-Mn mixed oxide (Co:Mn molar ratio of 1:3, samples D-F) thin films of various thickness (approximately 100. 200. and 300 mn) by RF magnetron sputtering and healed al 500 °C in air. The catalysts with various Mn content were examined by XRD, SEM, FUR. XPS, and Ih-TPR. tested in the gas-phase oxidation of model organic compound (ethanol) and compared with pelletized commercial Co-Mn- Al mixed oxide catalyst (Astin 2-100, Czech Republic, Co:Mn:Al molar ratio of 4:1:1 ). XRD measurements revealed no discrete Mn-containing phase in the deposited Co-Mn oxide layers, only Co.iOr. XPS analysis showed that Mn occurs mainly as MnO on the catalysts surface. According to T$o, ethanol oxidation proceeded slightly faster over the catalysts with thicker additional MnO coating. Additional coating of the deposited C03O4 layer with Co-Mn mixed oxide was not so effective in improvement of the catalysts activity. More precise evaluation of catalyst activity according to rzoo values (mmol of EtOH reacted over gram of active oxides per hour) slightly changed the order of reactivity: The catalyst with 100 nm MnO coaling over the CO3O4 was more active Ilian the others, very likely, because of intimate contact of CO3O4 and MnO. The Co/(Co-hMn) molar ratio around 0.25 provided the most active Co-Mn mixed oxide catalysts for ethanol oxidation. Simple MnOx catalyst showed lower temperature of T50, however, concentration of undesirable reaction byproduct, CO, was nearly two limes higher than those observed at the structured catalysts. Thus, MnO catalyzes oxidation of alcohols with high reaction rate but the rate of CO to CO2 oxidation is substantially lower than those observed al structured catalysis do. As compared with lhe pelletized Astin 2-100 catalyst, the temperatures required for 95 % conversion of ethanol to CO2 over the catalysts on stainless steel meshes were by 100 °C lower. The Astin 2-100 < at.thst did not exhibit the formation of CO, very likely, due to longer contact of i. j, umí i ompdiicnt with active sites in the catalyst pellets.

11* 4, m ir ul ill iiptxnlvil catalysts in the total oxidation of ethanol to CO: was i>f !,<. it,,,, in,i u| il» , omni, niai Astin 2-100 catalyst, though the content of active ■	i,, ,<i i,. i|,. i., ,I u( um lini-it t acilysis was more than 50 times lower.

\ . 1,	11 j. .,|l

fli an»' i hif i »*<• a I'.itt, i Hitifliifhifi lf>> ilk iiiiaiivi.il.support(pixject 17-08389S).

‘ ílh tyilk-:	4 '3. .,'0 B)